## CHARACTERISTICS

Hose made from thick transparent polyurethane compound reinforced by coppered galvanised steel.

Great flexibility and robustness, which provide it with large mechanical capabilities.

Anti-static.

Optimal resistance to abrasion, to environmental agents, and to a large range of chemical products

Temperature range between –35ºC and +85ºC

### USAGE

Suction and ducting of abrasive material, fumes, burrs, vapours, etc.

### TECHNICAL DATA

|  INT. mm | PESO g/m | ESPESOR De FLEXIBLE mm | ESPESOR De PARED mm | VACIO m H20 | RADIO CURVATURA mm |
| --- | --- | --- | --- | --- | --- |
| 40 | 230 | 0.4 | 1.8 | 5.0 | 40 |
| 51 | 280 | 0.4 | 1.9 | 4.0 | 50 |
| 60 | 340 | 0.4 | 2.0 | 3.0 | 60 |
| 70 | 390 | 0.4 | 2.0 | 2.0 | 70 |
| 76 | 410 | 0.4 | 2.0 | 2.0 | 76 |
| 80 | 440 | 0.4 | 2.0 | 1.5 | 80 |
| 90 | 490 | 0.4 | 2.0 | 1.5 | 90 |
| 102 | 510 | 0.5 | 2.3 | 1.5 | 100 |
| 110 | 560 | 0.5 | 2.3 | 1.5 | 110 |
| 120 | 610 | 0.5 | 2.3 | 1.5 | 120 |
| 125 | 630 | 0.5 | 2.3 | 1.5 | 125 |
| 130 | 660 | 0.5 | 2.3 | 1.5 | 130 |
| 140 | 760 | 0.5 | 2.3 | 1.5 | 140 |
| 152 | 790 | 0.5 | 2.3 | 1.0 | 150 |
| 160 | 880 | 0.5 | 2.3 | 1.0 | 160 |
| 180 | 950 | 0.5 | 2.3 | 1.0 | 180 |
| 203 | 1030 | 0.5 | 2.3 | 1.0 | 200 |
| 254 | 1475 | 0.5 | 2.6 | 1.0 | 250 |
| 300 | 1980 | 0.5 | 2.6 | 0.5 | 300 |
| 350 | 2000 | 0.5 | 2.6 | 0.5 | 350 |
| 406 | 2070 | 0.5 | 2.6 | 0.5 | 400 |

Rev. 29-10-2012